## Slide 1: Materials selection of the SPD Beam-Beam Counter scintillation detector prototype
М22-115
Zakharov A.M.
Preliminary Report
SPD MEPhI Group

## Slide 2
1
CAEN FERS-5200 readout system
FEE studies results
FERS-5200 is an extendable high speed front‐end readout system based on the DT5202 64-channel module for SiPM.
Concentrator DT5215 for the possibility of expanding the number of channels to 8192.
Citiroc 1A allows triggering down to 1/3 p.e. and provides the charge measurement with a good noise rejection. Moreover, Citiroc 1A outputs the 32-channel triggers with a high resolution timing (better than 100 ps).
Fine for testbeam and Phase0 experiments.
Main Acquisition Modes:
• SPECTROSCOPY.
• TIMING.
SPECT_TIMING. The Spectroscopy + Timing

## Slide 3
FEE studies results
PMT Hamamatsu H10720-110
The stand for BBC tile tests
Trigger time resolution ~650 ps
BC-404
2

## Slide 4
Materials selection (scintillator, optical cement, fibers, etc) and prototype tiles testing with material combinations.
Scintillator: Matte vs Tyvek covered
Optical cement: CKTN Med vs OK-72
Fibers: Saint-Gobain Crystals vs KURARAY
SiPMs: 3x3 mm2 ; 1x1 mm2
JINR and MEPhI Tests
Scintillation detector prototype materials
central
1 (L;R)
2 (L;R)
3 (L;R)
Line
3

## Slide 5
Calibration method (Led source)
FEE studies results
DT5202 with CAEN
LED Driver (SP5601)
4

## Slide 6
Matte and Tyvek comparison
FEE studies results
3 line tiles
1 line tiles
The result is similar, and due to the fact that the option with Tyvek carries the technological complexity of mass production, the option with matted one is more acceptable.
central
1 (L;R)
2 (L;R)
3 (L;R)
Line
5

## Slide 7
CKTN and OK-72 comparison
FEE studies results
CKTN and OK-72 Comparison Line 1
CKTN and OK-72 Comparison Line 3
CKTN and OK-72 Comparison Line 3 (old sample)
central
1 (L;R)
2 (L;R)
3 (L;R)
Line
6

## Slide 8
SG91AS, SG92S and Y-11 comparison
FEE studies results
WLS Comparison Line 3
central
1 (L;R)
2 (L;R)
3 (L;R)
Line
7

## Slide 9
Signal from central tiles
FEE studies results
Signal from central tiles, using different optical cements and WLS length
central
1 (L;R)
2 (L;R)
3 (L;R)
Line
8

## Slide 10
Central, line 1 and line 3 comparison
FEE studies results
Signals from central, line 1 and line 3 tiles seems to be different because of different fiber curvature (see tile system scheme)
9

## Slide 11
SG BCF92AS light collection
FEE studies results
Fit using pol1 function parameters
Difference between d1 and d4 for SG BCF91AS ≈ 5% of light collection
d1
d2
d3
d4
10

## Slide 12
3x3 and 1x1 calibration using 2 WLS tile
FEE studies results
Double WLS tile, used for calibration
11

## Slide 13
Thanks for attention!