## Slide 1
status BBC SPD @ JINR
Workgroups meeting, Moscow
October 2025
A.V.Tishevsky on behalf of JINR BBC workgroup
Notes: 1

## Slide 2
2
Introduction
BBC priorities
(Phase0)
Step 1-st
Selected options:
Scintillator: Uniplast-Vladimir (chemical mating)
Optical cement: CKTN Med mark B
WLS Fiber: Saint-Gobain Crystals (SG92S)
SiPM: SensL 1x1 mm2 (MicroFC-10035 SMTPA)
KURARAY (Y-11)
Final options for Phase ≥1
are:
Hamamatsu (S14160-1315PS)
BBC Sector (1/16 of wheel) design
Intermediate step
skill + changes (?)
(Phase1)
Step 2-nd

## Slide 3
Needs:
2 Wheels 128 scintillator tiles each
  -scintillator -yes
  -WLS – yes
  - SiPM – yes
DT5202 – yes
DT5215 – yes
Optical fiber – yes
Xe124+ target collisions (FT mode)
SPD Phase0
30% boronated polyethylene plates (ПБ-30)
for BBC/ZDC SPD
ООО «НПК Динамика»
(700х500х50 mm^3)
purchase is agreed
In progress
thanks to V. Poliakov
MPD pipe
Pipe (Al or Fe) (1.5 mm thick, 83 mm diameter)
targets (Au, Cu).
distance to collision point
talk by Volkov I.

## Slide 4
4
Proposal for reduced wheel prototype
BBC assembling part
Mass production issues:
R&D tests (+ mechanisms of verification)
Backplate
Connector for
WLS-to-clear fibers
Transmission box for
clear fibers to SiPMs
Front‐end
&
Readout
PC
for Phase0
CAEN FERS-5200
128 tiles (8x16)
reduced prototype wheel (x2)
(the 1-st priority)
WLS
8 ch
12 ch
NEW ELECTRONICS (needs)
for Phase ≥1
talk by Dubinin F.
talk by Solonbekov M.
talk by Nekrasov P.

## Slide 5
5
Sandwich backplate for BBC
BBC assembling part
thickness of each
~ 20 mm
I.
II.
I.
II.
I.
II.
Honeycomb
(3-options with
different thickness
of carbon layers)
Parts:
Infrastructure (grooved)
Detector support
The next steps are:
simulate the deformations of the backplate,
select main option.
The grooving map has been done.
728 x 728 mm2

## Slide 6
6
The sandwich backplate grooves for BBC
BBC assembling part
The grooving map
½ of wheel
the verification method has been implemented
the ability to quickly the connector substitution
Grooved wood backplate V.4.3
left output
right output

## Slide 7
7
The fiber laying
BBC assembling part
Длина, см | ряд | Длина, см
63 | 4 | 73.5
61.5 | 3 | 72.2
54.5 | 2 | 61.5
70 | 1 | 68
62 | 0 | 61
Reserve (min. 40mm)
Left/right output symmetry
The minimum diameters are the same
hard to transported

## Slide 8
8
The sandwich backplate grooves for BBC
BBC assembling part
the connector mounting is not reliable
WLS tension
not light shielded

## Slide 9
9
The sandwich backplate grooves for BBC
BBC assembling part
Grooved wood backplate
V.4.4 (final)
with uniform illumination (SGF)
kind of light-shielding tape (?)

## Slide 10
10
The sandwich backplate grooves for BBC
BBC assembling part
problem with tiles of neighboring sectors

## Slide 11
11
The mechanism of transported
BBC assembling part
https://1drv.ms/f/c/472043d3e6891bfc/ElejW62pvfVNpLCiogbmTfEBrmcCOR8yEwmVpFafLmUUkA?e=07G2Mb
shared models & etc.

## Slide 12
12
R&D
Mechanisms of verification
The verification for the mass production process
check the uniformity of the tiles
method for estimating the efficiency of an optical and electronic path
Method. Full-map (scintillator homogeneity, I) or coarse-grid X-ray scans (II).
For definition of:
defects
technological deviations (cement presence/quality, concentration; WLS turns)
Cement concentration (CKTN-E):
2.5/100 vs 3.2/100 (datasheet-recommended) → 24.6 vs 29.2 µA
(≈ 12%).
WLS turns (OK-72):
1 vs 3 → 14.5 vs 25.0 µA (≈ ×1.7).
The method based on side glow fiber (SGF).
(WLS <-> Clear Fiber <-> SiPM <-> DT5202 unit)
The distance from LED, cm
Mean, channels
Comparing of WLS
(3mm SGF diameter)
WLS Kuraray (Y11) is effective.
⌀3 mm is approved
fast method (immediately + the changes over time)+R&D
application for new backplate grooves design is required
Notes: 12

## Slide 13
13
Results
Current status
The details of BBC assembling part have been described.
The mechanism of transported have been proposed.
The verification for the mass production process have been proposed. The methods are promising.
To do list
modeling of the sandwich base hardness;
detailing the mechanics
finalizing the method of express sector check (NEW test samples + test of the upgraded optical cable and transmission box);
start the mass production process
Notes: 13

## Slide 14
14
Two full-size BBC sectors production
SPD Phase1
785.7
26 tiles
BBC Sector (1/16 of wheel) design
1/16 of reduced
prototype wheel
The version of FEE that uses KINTEX-7 FPGA and new analog part is under active development.
Analog part versions
V.1
V.2
XILINX VIRTEX-5 FPGA (current)
KINTEX-7 FPGA (new)

## Slide 15
Schedule of works
~ 5-7 months delay
15
Not JINR
full-size BBC sectors
~ 5-7 months delay
Notes: 15

## Slide 16
Thank you for the attention!

## Slide 17
Backup

## Slide 18
18
Introduction
Outline
Introduction
BBC assembling part
Hardware
R&D tests
Results (current status)
SPD Phase0 plans
  Simulation (Phase0)
SPD Phase1 plans

## Slide 19
Triggers of consecutive channels are sent to an AND logic operator (e.g. CH0&CH1, CH2&CH3, etc.). The 32 outputs are then sent to an OR logic operator.
Simplified block diagram of the DT5202 FERS‐5200 unit
Citiroc‐1A block scheme
Each channel has low (LG) and high (HG) gain preamplifiers providing a wide dynamic range.
Schematic view of the LED

## Slide 20
Calibration method (Led source)
Into TDR
Not calibrated
DT5202 with CAEN
LED Driver (SP5601)
The hardware of BBC tests part

## Slide 21
21
Scintillator cover
Materials selection test part
PMTs
Matted
or
Mylar
or
Tyvek
SensL SiPM (27.34 V.)
S.G. (WLS)
CKTN (opt. cement)
Cosmic rays
The option with matted tiles is more priority for mass production.
The “FersRun” framework has been designed.
The amplitude spectra of the BBC prototype scintillation tile coated with Mylar or Tyvek, as well as covered with Matted options.
Fited by convolution of Gauss and Landau functions “Langau”,
χ2 /NDF ~ 1.2
PMT Hamamatsu H10720-110
BC-404
External trigger by coincidence of two scintillators with PMTs readout

## Slide 22
22
Optical cement and WLS
Materials selection test part
The results of tests of Kuraray WLS fiber and Saint-Gobain Crystals (SGC) WLS fiber with different types of cement are presented.
CKTN mark B paired with SGC WLS fiber are the most appropriate candidates for prototype assembly tests.
CKTN mark B paired with Kuraray WLS fiber are the most appropriate candidates for future testbeam.
Light collection peak position on dependence of A component amount for optical cement.
CKTN
for
Prototype
tests
for
Phase 1
tests
Datasheet ratio will be used and closely monitored for mass production.

## Slide 23
23
Amplitude spectra of two sectors
Prototype assembling test
1-st sector prototype
2-nd sector prototype
There are 2 specific channels, but the debugging process of mass production continues.
The stable tiles were taken for following tests

## Slide 24
24
The 1-st step for working with the timing mode
Prototype assembling test
ToT correlations
LG correlations
The calibration of the charge scale is required
LG vs ToT (channel №3)
Correlation of energy deposition for 2 channels, as well as the time information for these channels.
ToT linearity.
CAEN [3]

## Slide 25
New FEE & Readout electronic
Simplified block diagram
The hardware for BBC
Front-end units
(SiPM supply, signal reading)
TDC based on FPGA (XILINX VIRTEX-5)

## Slide 26
Ch 0a
Ch 0
Ch 1a
Ch 2
Ch 1
Ch 2a
FERS
NE
V.2
“Majority (3ch) ”
Trigger logic
The hardware tests
The electronics test
Ch 2a
Ch 0a
Ch 1a
Tiles
Ch 2
Ch 0
Ch 1
FERS reference channel (Tref)
Ch 3
NE
NE
Channels
(x3)
Tref
ToT
ToT
Hybrid mode

## Slide 27
The hardware tests
Results
Ch 1
Ch 2
Ch 0
Ch 0
NE
Ch 2
Ch 0
Ch 1
Ch 0
LG, channels
TOT
LG vs ToT (channel 1)
Improvement the "FersRun" framework for the correlations between different electronic channels
Further research
NE improvements
are required
Analog part versions
(next V.3)
V.1
V.2
FPGA XILINX VIRTEX-5
FPGA KINTEX-7

## Slide 28
28
The optical cable prototype (clear fiber)
R&D tests
Schematic view of the LED
Light loss at 1 meter ~7%
Kuraray (clear fiber) cable prototype with 8 channels connector
SensL 3x3 mm2
(MicroFC-30035)
to DT5202
LED
tile
5 meters

## Slide 29
29
Application of DT5215 concentrator
SPD is planned to operate without T0 (start) so we need to work with free-streaming mode. (first step - Hybrid mode for DT5202)
Tref window
Hits acquisition ranges
Tref period
Tref delay
Tref may be provided by
- outer generator (T0)
- inner generator (PTRG)
Full range!
SPD Phase0
SiPM's array
Tests with SiPM’s array
Inner generator (Tref)
FERS
Data
Generator (signal)
LED
SiPM
Continuous data reading can be made only with fine-tuning of board parameters.
upgrade f/w and tests are required

## Slide 30
link[0]-unit[0]
link[1]-unit[1]
link[2]-unit[2]
link[0]-unit[0,1,2]
Generator (signal)
FERS
Data
Inner generator (Tref)
LINKS (1 & 0)
Concentrator to boards opto-fiber connection
DT5215 (FW v. 6.0 )
Tests with different unit-concentrator links configurations
Application of DT5215 concentrator

## Slide 31
The first stage of ZDC is – 6 planes + 1 veto with trapezoid geometry
Working on the beam BBC & ZDC (?)
  “FersRun” framework
  DT5215 concentrator
ZDC activities
SPD Phase0
DT5202 with 2X31 SiPM PLATES
was tested

## Slide 32
Mass production issues
32
Tiles and sectors: gluing frames
Prototype assembling part
The algorithm for polishing the connector has been proposed. The further developments are required:
Preparation of infrastructure for mass production (obtaining equipment, equipping rooms, etc.)
Development of methods of mass production (tools + algorithm)
mechanism working group BBC@MEPhI
tool working group BBC@JINR